Specification of Antistatic Fabric  (2/1 Twill)

	Warp Yarn
	Polyester 75D/36F

	Weft Yarn
	Polyester 100D/48F

	Conductive Yarn
	Carbon Yarn 97D/25F

	Weaving Structure
	2up/1down(Twill)

	Density (per inch)
	192 x 92

	Width (inch)
	60

	Weight (gr/㎡)
	119

	Conductive Yarn’s Interval
	5mm

	Air Permeability (cc/㎠.sec)
	9.4

	Moisture Permeability (gr/㎠.24hrs)
	7,122

	Frictional Static Charge (V)
	less 50

	Surface Resistivity (ohm/cm)
	10E6 

	Particle Efficiency (0.3㎛,%)
	80


